## Slide 1
STO(001) Characterization and Literature Review
Literature Review:
Found the most widely available RHEED images for STO(001) in available literature
Reconstructions include:
  (1 x 1)
  (2 x 1)
  (1 x 2)
  c(4 x 4)
  √13 x √13 R33.7°
  √13 x √13 + c(6 x 2) (superposition of two reconstructions)
Literature is often difficult to get ideal images from, due to differing MBE set ups and parameters across different labs
The result is that sometimes we get lower quality images than we are hoping for.

## Slide 2
(1 x 1), (2 x 1), √13 x √13(-R33.7°) + c(6 x 2)
(1 x 1)
Twinned(2 x 1)
Twinned √13 x √13(-R33.7°) + c(6 x 2)
Naito, Michio & Sato, Hisashi. (1994). Reflection high-energy electron diffraction study on the SrTiO3 surface structure. Physica C-superconductivity and Its Applications - PHYSICA C. 229. 1-11. 10.1016/0921-4534(94)90805-2.
Fig. 2. RHEED patterns of the SrTiO3(001 ) surfaces given different surface treatments. (a) as-polished surface, (b) vacuum-annealed surtace, and (c) oxygen-annealed surface with the [ 100] and [ 110] beam incidences.
Notes: This paper examines the RHEED images of different treatment types for STO along (001) and (110) crystal faces. Published in 1994, it is far from the most recent paper, but it also dives into the science of RHEED and the physical features that are reflected. Potentially useful for education purposes.

## Slide 3
(1 x 1), (1 x 2), c(4 x 4)
From: Surface reconstructions in molecular beam epitaxy of SrTiO3
Appl. Phys. Lett. 105, 191901 (2014)
(1 x 1)
c(4 x 4)
c(4 x 4)
(1 x 2)
Notes: This paper captures the changing RHEED patterns and therefore surface reconstructions as a function of TTIP/Sr. The first image corresponds to 37.5, second to 39.5, third to 45.0, and last to 60.0. These were all at T = 810 C.

## Slide 4
√13 x √13(-R33.7°)
(√13 x √13)R33.7°
Chong Liu, Kai Chang, Ke Zou; Realistic simulation of reflection high-energy electron diffraction patterns for two-dimensional lattices using Ewald construction. J. Vac. Sci. Technol. B 1 September 2022; 40 (5): 054002. https://doi.org/10.1116/6.0001899
Notes: In this paper, the authors use kinematic theory and Ewald construction to simulate the geometric transformations and the corresponding RHEED patterns.

## Slide 5
STO RHEED Simulation
In the paper Lui et al. J. Vac. Sci. Technol. B (2022), the authors introduced a software that uses RHEED kinematic theory to simulate realistic RHEED images
How it works:
Input real lattice unit cell
  Real space geometry
Transform into reciprocal space: real points  reciprocal lattice rods
Use Ewald Sphere construction to calculate diffraction conditions
Project intersections of sphere with rods onto screen
Result: simulated RHEED pattern derived from theory
Chong Liu, Kai Chang, Ke Zou; Realistic simulation of reflection high-energy electron diffraction patterns for two-dimensional lattices using Ewald construction. J. Vac. Sci. Technol. B 1 September 2022; 40 (5): 054002. https://doi.org/10.1116/6.0001899

## Slide 6
Simulation Parameters
STO(001) Reconstruction | (1 x1) | (2 x 1) | (2 x 1)/(1 x 2) | √13 x √13 (ideal) | √13 x √13 (from paper) | c(6 x 2) | √13 x √13 + c(6 x 2)
Number of Lattices | 1 | 1 | 2 | 2 | 2 | 1 | 3
Lattice base vectors: (x_1, y_1), (x_2, y_2) | (1,0), (0,1) | (2, 0), (0, 1) | (2,0), (0,1) | (2,3), (3,-2) | (2,3), (3,-2) | (6,0), (0, 2) | (2, 3), (3,-2)
 |  |  |  |  |  |  | (3,2), (2,-3)
 |  |  | (1,0), (0,2) | (3,2), (2,-3) | (3,2), (2,-3) |  | (6,0), (0,2)
Structure factors: (r_a, r_b, f) | (0, 0, 1) | (0, 0, 1) | (0,0,1) | (0,0,1) | (0,0,1) | (0, 0, 1) | (0, 0, 1)
 |  |  |  |  |  |  | (0, 0, 1)
 |  |  |  |  |  |  | (0, 0, 1) + (0.5, 0.5, 1)
Lattice Unit: (Å) | 3.905 | 3.905 | 3.905 | 3.905 | 3.905 | 3.905 | 3.905
Grazing Angle (°) | 3 | 3 | 3 | 3 | 2.6 | 3 | 3
Rotation (°) | 0 | 0 | 0 | 0 | 0 | 0 | 0
Beam E (keV) | 10 | 10 | 10 | 10 | 10 | 10 | 10
Broaden x, y | 1, 1 | 1, 1 | 1, 1 | 1, 1 | 0.8,0.7 | 1, 1 | 1, 1
Common Surface Reconstructions and their corresponding parameters in the software

## Slide 7
Simulated: (1 x 1) unreconstructed
STO(001) Reconstruction | (1 x1)
Number of Lattices | 1
Lattice base vectors: (x_1, y_1), (x_2, y_2) | (1,0), (0,1)
Structure factors: (r_a, r_b, f) | (0, 0, 1)
Lattice Unit: (Å) | 3.905
Grazing Angle (°) | 3
Rotation (°) | 0
Beam E (keV) | 10
Broaden x, y | 1, 1
Chong Liu, Kai Chang, Ke Zou; Realistic simulation of reflection high-energy electron diffraction patterns for two-dimensional lattices using Ewald construction. J. Vac. Sci. Technol. B 1 September 2022; 40 (5): 054002. https://doi.org/10.1116/6.0001899

## Slide 8
Side by Side: (1 x 1) unreconstructed
Chong Liu, Kai Chang, Ke Zou; Realistic simulation of reflection high-energy electron diffraction patterns for two-dimensional lattices using Ewald construction. J. Vac. Sci. Technol. B 1 September 2022; 40 (5): 054002. https://doi.org/10.1116/6.0001899

## Slide 9
Simulated: √13 x √13(-R33.7°)
STO(001) Reconstruction | √13 x √13 (from paper)
Number of Lattices | 2
Lattice base vectors: (x_1, y_1), (x_2, y_2) | (2,3), (3,-2)
 | (3,2), (2,-3)
Structure factors: (r_a, r_b, f) | (0,0,1)
Lattice Unit: (Å) | 3.905
Grazing Angle (°) | 2.6
Rotation (°) | 0
Beam E (keV) | 10
Broaden x, y | 0.8,0.7
Chong Liu, Kai Chang, Ke Zou; Realistic simulation of reflection high-energy electron diffraction patterns for two-dimensional lattices using Ewald construction. J. Vac. Sci. Technol. B 1 September 2022; 40 (5): 054002. https://doi.org/10.1116/6.0001899

## Slide 10
Side by Side: √13 x √13

## Slide 11
Simulated: √13 x √13(-R33.7°) + c(6 x 2)
STO(001) Reconstruction | √13 x √13 + c(6 x 2)
Number of Lattices | 3
Lattice base vectors: (x_1, y_1), (x_2, y_2) | (2, 3), (3,-2)
 | (3,2), (2,-3)
 | (6,0), (0,2)
Structure factors: (r_a, r_b, f) | (0, 0, 1)
 | (0, 0, 1)
 | (0, 0, 1) + (0.5, 0.5, 1)
Lattice Unit: (Å) | 3.905
Grazing Angle (°) | 3
Rotation (°) | 0
Beam E (keV) | 10
Broaden x, y | 1, 1
Chong Liu, Kai Chang, Ke Zou; Realistic simulation of reflection high-energy electron diffraction patterns for two-dimensional lattices using Ewald construction. J. Vac. Sci. Technol. B 1 September 2022; 40 (5): 054002. https://doi.org/10.1116/6.0001899

## Slide 12
Side by Side: √13 x √13(-R33.7°) + c(6 x 2)
Chong Liu, Kai Chang, Ke Zou; Realistic simulation of reflection high-energy electron diffraction patterns for two-dimensional lattices using Ewald construction. J. Vac. Sci. Technol. B 1 September 2022; 40 (5): 054002. https://doi.org/10.1116/6.0001899

## Slide 13
Simulation Caveats
Realistic Limitations of this software:
No Kikuchi lines
  These come about from inelastic scattering, the simulation removes them
Idealized RHEED streaks
  In experimental settings these streaks are often stretched due to various surface conditions
File format
  These images are generated as .png’s, whereas the actual RHEED images are usually stored as .bmp’s
Parameter Uncertainty
  Some of the parameters used in the software do not exactly correspond to the actual MBE set up in lab (ex. Grazing angle)
Not suitable replacement for real data
  Helpful to have for what is ‘theoretically’ possible, but often does not resemble realistic RHEED images without having to tweak parameters
Naito, Michio & Sato, Hisashi. (1994). Reflection high-energy electron diffraction study on the SrTiO3 surface structure. Physica C-superconductivity and Its Applications - PHYSICA C. 229. 1-11. 10.1016/0921-4534(94)90805-2.

## Slide 14
Subtask: STO characterization
√13 x √13(-R33.7°)
Lui et al. Method
Ideal* simulation
Our group
Lui et al. RHEED
Chong Liu, Kai Chang, Ke Zou; Realistic simulation of reflection high-energy electron diffraction patterns for two-dimensional lattices using Ewald construction. J. Vac. Sci. Technol. B 1 September 2022; 40 (5): 054002. https://doi.org/10.1116/6.0001899

## Slide 15
Subtask: STO characterization
Hiroyuki Tanaka et al 1993 Jpn. J. Appl. Phys. 32 1405
√5 x √5-R26.6°
Notes: This paper was published in 1993. This image was taken at 1200 C in UHV for 2 minutes.

## Slide 16
Subtask: STO characterization
Surface Structures of SrTiO3 (001): A TiO2-rich Reconstruction with a c(4 × 2) Unit Cell
Natasha Erdman, Oliver Warschkow, Mark Asta, Kenneth R. Poeppelmeier, Donald E. Ellis, and Laurence D. Marks
Journal of the American Chemical Society 2003 125 (33), 10050-10056
DOI: 10.1021/ja034933h
Notes: I couldn’t find a RHEED image for c(4 x 2) reconstruction, but this paper from 2003 discusses the surface of STO in depth

## Slide 17
Subtask: STO characterization
(1 x 2) [100]
From: Surface reconstructions in molecular beam epitaxy of SrTiO3
Appl. Phys. Lett. 105, 191901 (2014)
Chong Liu, Kai Chang, Ke Zou; Realistic simulation of reflection high-energy electron diffraction patterns for two-dimensional lattices using Ewald construction. J. Vac. Sci. Technol. B 1 September 2022; 40 (5): 054002. https://doi.org/10.1116/6.0001899

## Slide 18
Subtask: STO characterization
c(6 x 2) (HTR)
Chong Liu, Kai Chang, Ke Zou; Realistic simulation of reflection high-energy electron diffraction patterns for two-dimensional lattices using Ewald construction. J. Vac. Sci. Technol. B 1 September 2022; 40 (5): 054002. https://doi.org/10.1116/6.0001899

## Slide 19
Subtask: STO characterization
(2 x 1) [100]
Chong Liu, Kai Chang, Ke Zou; Realistic simulation of reflection high-energy electron diffraction patterns for two-dimensional lattices using Ewald construction. J. Vac. Sci. Technol. B 1 September 2022; 40 (5): 054002. https://doi.org/10.1116/6.0001899

## Slide 20
Subtask: STO characterization
√13 x √13(-R33.7°)
Lui et al. Method
Ideal* simulation
Chong Liu, Kai Chang, Ke Zou; Realistic simulation of reflection high-energy electron diffraction patterns for two-dimensional lattices using Ewald construction. J. Vac. Sci. Technol. B 1 September 2022; 40 (5): 054002. https://doi.org/10.1116/6.0001899